## Bridge Deck
(October 1995)

| Project No. | Date |
| --- | --- |
| Reviewer | % Work Complete % Time Elapsed |
| In Company with: Note: References are "Portland Cement Concrete" Section 505 "Concrete Structures" Section 506 |  |

Specification Requirements

| Concrete Mix Temperature ______________ ° F min. | ______________° F max. |
| --- | --- |
| Air Content%______________ to | ______________ % |
| Slump (no water reducer) ______________ inches to | ______________ inches |
| Slump (water reducer) ______________ inches to | ______________ inches |
| W/C Ratio ______________ Gals/bag, | ______________ lbs/lbs |
| Strength ______________ psi(min.) |  |

Plant Site

- Which coarse aggregate gradation was selected? Check gradation results for both coarse and fine aggregates (505.2.2, p 301 and 505.2.3, p.302).

- Is the combined minus 200 less than 1.75% (505.2.3.4, p.303)?

- Does the coarse aggregate gradation meet the maximum size aggregate requirement(s) (505.3.1.1, p.305)?

- Has a mix design been submitted and approved (505.3.2, p.307)?

- Is Type II cement being used (505.2.1, p.300)?

- Is fly ash being used? Is it from an approved source? Has maximum replacement been followed (15%) using the replacement ratio specified (1.25:1)? (505.2.5.4, p.303 and 304)

- Are there adequate supplies of aggregate both coarse and fine (505.3.11.8, p.314)?

- Have batch plant scales been certified (505.3.4.1, p.309)?

- Are air-entraining agents and other approved admixtures added to water before it enters the mixer (505.3.4.4, p.309)?

- When using two admixtures, are they kept separate so they will not be in contact prior to entering the mixing drum (505.3.4.4, p.309)?

- Mixing - stationary mixers should have 80 seconds mixing time (505.3.4.5, p.309), and truck mixers should mix for 70 to 100 revolutions (505.3.4.8, p.309) and a minimum of 90 revolutions for front-end discharge trucks (505.3.4.8, p.309)?

- Are transit mixer trucks properly equipped with water meters and revolution counters (505.3.6.2, p.311)?

- W/C ratio shall not exceed the maximum specified. Is the W/C ratio being monitored? Has the W/C ratio been exceeded (505.3.6.3, p.311)?

- If fly ash is used, has the cement been introduced into the mixer before the fly ash (505.3.4.5, p.309)?

- If heated, the mixing water shall be heated to a temperature of not less than 70 ° F nor more than 150 ° F when introduced into the mixer (505.3.5.6, p.310)?

Remarks

Project Site

- Are forms properly placed and secure? Has the reinforcing steel been properly placed (506.3.1.2 and 506.3.2, p.317)?

- Are the forms clean and oiled (506.3.2.6 and 506.3.2.7, p.318)?

- When sampled on the deck, is the sample taken from a small pile placed in the same manner as the normal operation in front of the deck screed? Has all the grout been pumped out? (505.3.9.1, p.312)

- Has minimum sampling and testing frequency been met (air content, slump, and strength - one per 50 yd3 of concrete from Table 505-6, p.312 and section 505.3.11.4, p.314)? Has the start-up frequency and frequency after failures been met (505.3.11.3, p.314)?

- Has an adequate storage device for test cylinders been provided at least 24 hours before concrete placement? Has it been checked out (505.3.9.2, p.312)?

- If transit mixer trucks are used, is water added after leaving the plant? Has the W/C ratio been exceeded? If water is added, has concrete been mixed for 30 revolutions (505.3.6.3, p.311)?

- Water shall not be added after 2 CY of concrete has been discharged (505.3.6.3, p.311).

- Has concrete been placed within 90 minutes for temperatures below 80°F and 60 minutes if the temperature is above 80 °F (505.3.7.2, p.311)?

- Is the concrete temperature between 50° F and 90 °F (60 ° F and 90 ° F for cold weather concreting - 506.3.9.2, p.324) at time of placement (505.3.8, p.311)?

- Has curing compound been applied at an appropriate time (within 20 minutes of the tining operation - 506.3.14.1, p.332)?

- Has the surface been textured as specified (1/8 inch-wide, 1/8 inch deep, and spaced randomly from 2 to 3/4 inch - 506.3.13.9, p.332)?

- Has the deck been straight-edged during the deck placement (506.3.13.8, p.331)?

- Review results of air content and slump for compliance with the specifications (Table 505-5, p.305).

Remarks