State Highway Transportation Department

Bridge Construction

# Post-Placement Inspection Checklist

- Inspection of steel stay in place deck forms

- After a minimum of two days of curing, inspect the forms for soundness and bonding per state specification xxx.

- Straightedging (spec. ref.)

- Inspect bridge deck and approach slab surface.  It should not vary by more than 4 mm (1/8 inch) measured from bottom of straightedge.

- Vertical steps at ends of decks and approach slabs shall not exceed 5 mm (3/16 inch).

- Expansion joints shall be placed from 2 to 5 mm (1/16 inch to 3/16 inch) below grade.

- Inspect entire deck for excess roughness, plastic shrinkage cracking, or surface tearing.

- Correct deficiencies per spec ref.

- Grooving Hardened Concrete

- After straightedging and repair, the deck shall be grooved.

- Width of grooves shall be 3mm +/- 0.5mm.

- Depth of grooves shall be 3 to 6 mm (1/8” to 1/4”).

- Longitudinal grooves shall be spaced at 19mm center to center (approx. ¾”) constant spacing.

- Transverse grooves shall have variable spacings from 13 to 22 mm (approx. ½” to 7/8”).

- Removal of slurry shall be continuous and immediate.

- Penetrating Water Repellent

- After grooving, and after the concrete has achieved design strength, verify bridge decks and approach slabs receive a penetrating water repellent treatment. (spec ref.)

E.	Sealing of Construction Joints and Cracks

- After grooving and after applying the penetrating water repellent, Verify all construction joints and cracks visible on a dry deck have been sealed with appropriate materials (spec ref)